| UNIVERSITY OF NIŠ |
| --- |
| Course Unit Descriptor | Faculty | Faculty of Mechanical Engineering |
| GENERAL INFORMATION |
| Study Program | Mechanical Engineering |
| Study Module (if applicable) | - |
| Course Title | Technical materials |
| Level of Study | ☒Bachelor | ☐ Master’s | ☐ Doctoral |
| Type of Course | x Obligatory | Elective |
| Semester | Autumn | x Spring |
| Year of Study | I |
| Number of ECTS Allocated | 6 |
| Name of Lecturer/Lecturers | Assoc. Prof. Goran Radenković and Assoc. Prof Gordana Stefanovic |
| Teaching Mode | ☒ Lectures | ☐ Group tutorials | ☐ Individual tutorials |
|  | ☒ Laboratory work | ☒ Project work | ☒ Seminar |
|  | ☐ Distance learning | ☐ Blended learning | ☐ Other |
| Purpose and Overview (max. 5 sentences) |
| Introduce students to the basics principles in the area of fuels, lubricants and industrial water as well as for managing in the systematization and terminology in practice. To familiarize students with basic types of materials used in mechanical engineering, their structure, properties, application and processing possibilities and changes their properties. |
| Syllabus (brief outline and summary of topics, max. 10 sentences) |
| 1) General introduction to technical materials, 2) Eenergy supply, reserves and consumption, 3) Fuel and fundamentals of combustion, 4) Solid fuel, 5) Liquid fuels, 6) Gaseous fuels, 7) Lubricants and their role in mechanical engineering, 8) General classification and the choice of type of lubricant, 9) Industrial water, 10) Crystalline materials. The structure diagrams Fe-Fe3C and Fe-C. 11) Mechanical, technological and non-destructive testing. 12) Steels. 13) Carbon and alloyed steel. 14) Structural, tool and steels special purposes. 15) Cast iron. 16) Non-ferrous alloys. 17) Ceramic materials. 18) Composite materials. 19) The choice of material from the standpoint of properties, processability, availability, price, etc.. |
| Language of Instruction |
| ☒Serbian (complete course) | English (complete course) | ☐ Other _____________ (complete course) |
| ☐Serbian with English mentoring | ☐Serbian with other mentoring ______________ |
| Assessment Methods and Criteria |
| Pre exam Duties | Points | Final Exam | Points |
| Activity During Lectures | 5 | Written Examination | 50 |
| Practical Teaching | 10 | Oral Examination | Max. 35 (depending on Teaching Colloquia) |
| Teaching Colloquia | 35 | Overall Sum | 100 |
| *Final examination mark is formed in accordance with the Institutional documents |